GUIDELINES — ASPHALT PROJECTS (PLANT MIX ONLY).  WHEN THIS PROVISION APPLIES INCLUDE THE FOLLOWING IN THE PROPOSAL: S515B03 Cold Planing Asphalt Operations, SS51505 Planing or Milling Pavement, S315LM2 Sur Prep-Restore -Before Overlay, S315SM1 Seal Crack ACP-HCCP-Bef Ovrly, S315QM1 Mainline Overlay Limits at Intersect.

S315AE0-1215

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

ASPHALT CONCRETE SCRATCH/LEVELING COURSE PRIOR TO PLANT MIX OVERLAY

September 24, 2015

I.	DESCRIPTION

This work shall consist of scratching and/or leveling a crack sealed, scabbed or distorted pavement surface (milled or unmilled) with the appropriate asphalt mixes in areas designated by the Engineer.  This work is applicable only to the routes or areas designated to be overlaid in this contract and where the Engineer has authorized the limits for scratching/leveling.  This work will be accomplished prior to the overlay paving operation.  After the scratching/leveling, the Contractor will be responsible for maintaining the prepared surface until the overlay has been completed.

Definitions: For the purpose of the Specifications surface preparation is defined as the following:

TYPE I -	A localized scratch/level of the pavement, including crack sealed, distorted or scabbed areas, no more than 50 percent of the surface area to be overlaid in each distinct paving site/location on the contract.

TYPE II -	A widespread scratch/level of the pavement, including crack sealed, distorted or scabbed areas, more than 50 percent of the surface to be overlaid in each distinct paving site/location on the contract.

II.	MATERIALS

Asphalt concrete scratch and/or leveling material shall be the surface mix asphalt designated in the contract or as approved by the Engineer.  SMA should not be used as a scratch/leveling course material.  Limestone mixes (L) may be used in leveling courses when approved by the Engineer.

Tack coat shall conform to the requirements of Section 210 of the Specifications and be the same material as used for the final surface course.

III.	PROCEDURES

For surfaces that will receive a direct overlay, the Engineer will designate the limits of surface area for scratch/leveling course to be achieved prior to beginning the work. For pavements that are milled, the Engineer will identify and designate the limits of surface area for scratch/leveling course to be placed as the work progresses, with communication(s) frequency and method(s) agreed upon before the work begins.

Areas designated for scratch/leveling course shall be thoroughly cleaned prior to applying tack coat.

A tack coat shall be applied to all exposed surfaces of the area which will receive asphalt material in accordance with Section 310 of the Specifications.

The Contractor shall utilize the mix and type of asphalt for scratch/leveling course in accordance with Section II Materials that he shall use with that route’s overlay unless otherwise approved by The Engineer.  Asphalt material shall be placed in a lift of no more than 2 inches in depth; typical lifts are approximately 1 inch in depth.  After each lift, it shall be compacted with equipment in accordance with Section 315.03(c) using a minimum of 3 passes of a minimum 8 ton roller.  Density testing will not be required.  Care shall be taken to ensure the surface of the finished repaired area conforms to the grade of the surrounding pavement.

IV.	MEASUREMENT AND PAYMENT

When the bid proposal contains a pay item, corresponding to any of the types below, specified in the “Schedule of Items”; that type of scratch/leveling course will include the work designated in the corresponding type’s description and be paid for in accordance with the price designated by the bidder.  If the bid proposal contains no pay item for the type of scratch/leveling course as described herein, such as may be discovered in the field; that scratch/leveling course shall meet the definition of Section I and will be measured and paid for in accordance with the following:

Scratch/Leveling Course Type I will be measured in tons of asphalt material and paid for at the rate of two times the contract unit bid price per ton of the mix type(s) of asphalt authorized by the Engineer.  This price shall include preparing the area, furnishing and applying tack coat, furnishing and applying asphalt material, and compaction.

Scratch/Leveling Course Type II will be measured in tons of asphalt material and paid for at the rate of one and one-half times the contract unit bid price per ton of the mix type(s) of asphalt authorized by the Engineer.  This price shall include preparing the area, furnishing and applying tack coat, furnishing and applying asphalt material, and compaction.

When included in the “Schedule of Items”, payment will be made under:

| Pay Item |  | Pay Unit |
| --- | --- | --- |
| Scratch/Level Type I |  | Tons |
| Scratch/Level Type II |  | Tons |