GUIDELINES —PROJECTS REQUIRING REGULAR OR NON-TRACKING TACK.

SS31001-1215                                                                                                             December 4, 2015

VIRGINIA DEPARTMENT OF TRANSPORTATION

2007 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SUPPLEMENTAL SECTION 310—TACK COAT

SECTION 310—TACK COAT of the Specifications is completely replaced with the following:

310.01—Description

This work shall consist of preparing and treating an existing asphalt or concrete surface with asphalt in accordance with these specifications and in conformity with the lines shown on the plans or as established by the Engineer.

310.02—Materials

- Tack Coat asphalt tack coat shall be CQS-1h, CRS-1h, or CSS-1h conforming to Section 210 of the Specifications.  Asphalt emulsion CMS-2 conforming to Section 210 of the Specifications may be used during the winter months.

(b)	Non-Tracking Tack Coat liquefied asphalt shall be selected from the Materials Division Approved Products List 50.1A.  The Contractor shall not dilute non-tracking tack coat materials with water.

310.03—Procedures

The existing surface shall be patched, cleaned, and rendered free from irregularities to the extent necessary to provide a reasonably smooth and uniform surface.  The Contractor shall remove unstable corrugated areas, and replace with suitable patching materials when required by the contract specifications.  The Contractor shall clean the edges of existing pavements that are to be adjacent to new pavement to permit adhesion of asphalt.

The Contractor shall uniformly apply tack coat or non-tracking tack coat material with a pressure distributor conforming to Section 314.04(b) of the Specifications.  Hand spray equipment shall not be used except in areas inaccessible by a pressure distributor.

The distributor shall be calibrated by the Contractor in the presence of the Engineer prior to initial asphalt plant mix placement to demonstrate an even and accurate spray application.  Calibration will be considered acceptable when the spray rate is uniform and within 0.02 gallon per square yard of the design application rate.

All tack coat and non-tracking tact coat materials stored longer than 30 days from the shipping date on the Bill of Lading shall be retested in accordance with Section 210.06 of the Specifications to verify the material still meets product specifications.

Tack at joints, adjacent to curbs, gutters, or other appurtenances shall be applied with a hand wand or with spray bar at the rate of 0.2 gallon per square yard. At joints, the tack applied by the hand wand or a spray bar shall be 2 feet in width with 4 to 6 inches protruding beyond the joint for the first pass.  Tack for the adjacent pass shall completely cover the vertical face of the pavement mat edge so that slight puddling of asphalt occurs at the joint, and extend a minimum of one foot into the lane to be paved.

Care shall be taken to prevent spattering adjacent items during the application of tack coat.  The distributor shall not be cleaned or discharged into ditches or borrow pits, onto shoulders, or along the right of way.

When not in use, the Contractor shall ensure equipment is parked so that the spray bar or mechanism will not drip asphalt on the surface of the traveled way.

The tack coat or non-tracking tack coat shall be applied to the pavement surface in such a manner that it will bond the overlay and the underlying surfaces together.

The Contractor shall apply tack coat and non-tracking tack coat in accordance with the weather limitations that apply to the course being placed as well as the manufacturer’s recommendations.  The Engineer will verify, and reserves the right to alter, the quantity, rate of application, temperature, and areas to be treated prior to application.

The tack coat or non-tracking tack coat shall be applied in a manner to offer the least inconvenience to traffic and to permit one-way traffic without pick up or tracking of the asphalt onto adjacent non-treated areas.  All traffic, including construction traffic, shall be excluded from tacked sections until the tack has cured.

Tack shall not be required atop asphalt stabilized open-graded material drainage layers.

The contractor shall measure and report to the agency on forms provided by the Engineer, the rate of tack material applied on a daily basis using VTM-137 Method B (Tack Yield Method).

The Engineer shall verify the desired tack application rate is achieved using VTM-137 Method A (Tack Plate Method).  This test shall be performed at a minimum frequency of once per each roadway, within the first 500 tons of asphalt mix placed, unless otherwise approved by the Engineer.

The Engineer reserves the right to perform the tack plate method testing at a higher frequency, as determined necessary, to ensure adherence to specifications.

(a)	Tack Coat

Equipment for heating and applying asphalt shall conform to Section 314.04(b) of the Specifications. The maximum application temperature of liquid asphalt shall conform to Table III-1.

TABLE III-1

Liquid Asphalt Application Temperature

|  | Type | Max. Temperature (oF) |
| --- | --- | --- |
|  | RC-70 | 180 |
|  | RC-250 | 220 |
|  | RC-800 | 225 |
|  | RC-3000 | 290 |
|  | MC-70 | 180 |
|  | MC-250 | 220 |
|  | MC-800 | 255 |
|  | MC-3000 | 290 |
|  | AC-5 | 300 |
|  | AC-10 | 300 |
|  | AC-20 | 300 |
|  | AC-40 | 300 |
|  | RS-2 | 175 |
|  | SS-1h | 180 |
|  | AE-4 | 150 |
|  | CRS-2 | 175 |
|  | CSS-1h | 180 |
|  | CMS-2 | 200 |
|  | CRS-1h | 175 |
|  | CRS-1 | 175 |
|  | CQS-1h | 180 |

The Contractor shall apply asphalt at the rate of 0.05 to 0.10 gallons per square yard.

The Contractor shall allow the tack coat to properly cure and break before placement of the hot mix asphalt course.

(b)	Non-Tracking Tack Coat

The Contractor shall apply non-tracking tack coat between May 1 and October 1.  The Contractor may use tack coat as specified herein at other times.

Equipment for heating and applying asphalt shall conform to Section 314.04(b) of the Specifications or the non-tracking tack coat material’s manufacturer’s recommendations.  The maximum application temperature of liquefied asphalt shall conform to the manufacturer’s requirements.

The Contractor shall apply tack material at the rate recommended by the manufacturer.  This rate is typically between 0.05 to 0.10 gallons per square yard.

Adjacent concrete or asphalt concrete surfaces shall show minimal visible evidence and white or yellow pavement markings shall show no visible evidence of the asphalt tack material tracking at the end of the production shift.  Tracking of the tack material on pavement markings will require the Contractor to restore the marking to their original pre-tack condition.  The Contractor shall remove Build-up of the tacking material on existing pavement surfaces.

(c)	Referee System

When a new asphalt course is placed on a milled or non-milled surface, the Contractor shall take steps to ensure an adequate bond is made between the new material and the existing surface. If the Engineer suspects the Contractor is failing to apply good bond promoting procedures or adequately tacking the existing surface per the manufacturer’s recommendations, the Engineer may core a minimum of 10 locations to determine the shear and tensile strength at the interface.

The Engineer will determine these locations by using a stratified random selection process.  The Department will test cores in the Department’s laboratory in accordance with VTM-128.  For the surface to be acceptable, the average results for shear and tensile strength specified herein must be met.  The Department will test a minimum of 5 cores for shear strength and at least 5 cores for tensile strength.

1.	Milled surfaces: The average shear strength must meet or exceed 100 psi with no single core having a shear strength less than 50 psi. The average tensile strength of the remaining cores must meet or exceed 40 psi with no single core having a tensile strength less than 20 psi.

2.	Un-milled surfaces: The average shear strength must meet or exceed 50 psi with no single core having a shear strength less than 30 psi. The average tensile strength of the remaining cores must meet or exceed 30 psi with no single core having a tensile strength less than 20 psi.

The Engineer will reduce the payment for the asphalt concrete tonnage placed in the area of dispute by 10 percent if the minimum shear or tensile strength requirements in that area are not met.

310.04—Measurement and Payment

Tack coat, including Tack Coat and Non-Tracking Tack Coat materials, when a pay item, will be measured in gallons and will be paid for at the contract unit price per gallon.

On a daily basis, the Contractor shall provide the Engineer readings taken from the calibrated distributor establishing the quantity of gallons placed for that day.  Quantity for payment will be based on volume and temperature corrections in accordance with Section 109 of the Specifications.

When not a pay item the Contractor shall include the cost in the contract unit price for other appropriate items.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Tack coat | Gallon |