GUIDELINES — FOR PROJECTS REQUIRING PAVEMENT MARKINGS OR MARKERS.

SS70402-0815                                                                                                                April 15, 2015

VIRGINIA DEPARTMENT OF TRANSPORTATION

2007 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SUPPLEMENTAL SECTION 704—PAVEMENT MARKINGS AND MARKERS

SECTION 704—PAVEMENT MARKINGS AND MARKERS of the Specifications is amended as follows:

Section 704.02—Materials is amended to include the following:

All pavement markers and pavement marking materials shall be selected from the VDOT Materials Division Approved Products List

Section 704.03—Procedures is amended to replace the second sentence of the second paragraph with the following:

Pavement markings installations, including symbol/message markings, shall be completed within the time limits herein on roadways where the pavement markings have been removed or obscured and the roadway is reopened to traffic, unless otherwise directed by the Engineer.

Section 704.03—Procedures is amended to replace the third through fifth paragraphs with the following:

Pavement marking installation on interstates, and other freeways (fully limited-access divided roadways with two or more lanes per direction) with posted speed limit of 55 mph and greater, , shall be completed within the workday during which the pavement markings were removed, eradicated, or obscured prior to reopening the lanes to traffic.

Pavement marking installation on non-freeway roads having traffic volumes of 10,000 ADT or more shall be completed within 24 hours after the end of the workday on which the existing pavement markings were removed, eradicated, or obscured.

Pavement marking installation on non-freeway roads having traffic volumes between 3,000 and 10,000 ADT shall be completed within 48 hours after the end of the workday on which the existing pavement markings were removed, eradicated, or obscured.

Pavement marking installation on non-freeway roads having traffic volumes of less than 3,000 ADT shall be completed within 72 hours after the end of the workday on which the existing pavement markings were removed, eradicated, or obscured.

Section 704.03(a) Pavement Markings is amended to replace the seventh through eleventh paragraphs with the following:

Pavement message/symbol markings shall be installed using Type B Class I, II, or IV markings unless indicated otherwise in the contract documents and shall include, but not be limited to school zone markings, railroad crossing markings, accessible (disabled) parking symbols, turn lane (elongated) arrows, word messages, etc.

The Contractor shall protect the public against potential damages that may result from pavement marking operations.  The Contractor shall be responsible for the complete preparation of the pavement surface, including, but not limited to, removing dust, dirt, loose particles, oily residues, curing compounds, concrete laitance, residues from eradication, and other foreign matter immediately prior to installing pavement markings.  The pavement surface shall be dry when tested in accordance with VTM-94 at the time of permanent pavement marking installation.  The Contractor shall be responsible for providing the apparatus indicated in VTM-94 that are needed to perform the moisture test.

Liquid markings shall be applied so as to prevent splattering and overspray, and shall be protected from traffic until track free by the use of traffic control guarding or warning devices as necessary.  If a vehicle crosses a pavement marking and tracks it, or if splattering or overspray occurs, the affected marking and resultant tracking, overspray or splattering shall be immediately eradicated, the affected pavement and other surfaces cleaned and prepared, and new markings applied at the Contractor’s expense.

Equipment shall be thoroughly cleaned between changes in colors or types of materials.

Pavement markings shall have clean and well-defined edges without running, bleeding or deformation.  Markings shall be uniform in appearance, free of waviness; (the edge of the marking not varying more than 1/4 inch in three feet from a straight line or more than one inch in fifty feet for a maximum distance of 500 feet) shall be straight on tangent alignment; and shall be on a true arc on curved alignment.

The widths of pavement markings shall not deviate more than 1/4 inch on tangent sections, nor more than 1/2 inch on curves from the required width.  The length of the gap and the length of the individual stripes that form skip lines shall not deviate more than two inches from their required lengths.  The length of the gap and individual skip line shall be of such uniformity throughout the entire length of each that a normal striping machine shall be able to repeat the pattern and superimpose additional striping upon the existing marking.

Glass beads shall be applied at the rate specified herein and shall be evenly distributed over the entire surface of the marking.  The Contractor shall apply beads to the surface of liquid markings with a bead dispenser attached to the applicator that shall uniformly dispense beads simultaneously on and into the just-applied marking.  The bead dispenser shall be equipped with a cut-off control synchronized with the applied marking material cut off control so that the beads are applied totally on the marking.  Beads shall be applied while the liquid marking is still fluid.  Approximately 70 percent of the beads shall be buried in the marking, and the remaining 30 percent shall be 50 to 60 percent embedded in the marking’s surface, unless otherwise specified by the pavement marking manufacturer.  Beads installed on crosswalks and stop lines on roadways with curbs only (no gutter) may be hand applied for two feet at the end of each line next to the curb with 100 percent of the beads embedded 50 to 60 percent into the marking’s surface.

The Contractor shall provide written certification that all preformed symbols/characters, or the templates used to create such symbols/characters for non-preformed markings, match the size and shape specified in the VDOT Road And Bridge Standards and the contract documents.

Section 704.03(a)2 Type B Markings is amended to replace the second paragraph with the following:

Non-truck mounted equipment for application of thermoplastic material shall be of the screed extrude type with a screw-drive or shall be self-propelled and regulated to allow for calibration of the amount of material applied.  Non-truck mounted equipment for application of epoxy resin material shall also be self-propelled and regulated to allow for calibration of the amount of material applied.

Section 704.03(a)2a Thermoplastic (Class I) is replaced with the following:

Thermoplastic (Class I) material shall be applied by screed extrusion, ribbon gun, or spray equipment.  Alkyd thermoplastic may be applied directly after the paving operations; however, hydrocarbon thermoplastic shall not be applied less than 30 days after the paving operations.

Alkyd and hydrocarbon materials shall not be mixed together.  The Contractor shall ensure equipment is thoroughly cleaned when colors or types of material are changed.

Thermoplastic shall not be applied over existing pavement markings of other materials unless the existing marking is 90 percent worn away, obscured, or eradicated.  Thermoplastic shall only be applied over existing thermoplastic markings if the existing thermoplastic markings are clean and not chalky, chipped or powdery in appearance or condition.

Section 704.03(a)2b Polyester Resin (Class II) is replaced with the following:

Preformed Thermoplastic (Class II) material shall be installed per the manufacturer’s recommendations.  When markings are installed on hydraulic cement concrete pavement, primer shall be applied first in accordance with manufacturer’s requirements.

Additional glass beads shall be applied evenly to the surface of the preformed thermoplastic material for messages and symbols immediately after installation at the rate of 7 pounds per 100 square feet to facilitate embedment while the material is in a softened state using manufacturer approved equipment, bead package, and methods.

Section 704.04—Measurement and Payment is amended to replace paragraphs two and three with the following:

Pavement message markings will be measured in units of each or linear feet and will be paid for at the contract unit price per each per location or linear foot as applicable for the size and/or type and class specified.  This price shall include the pavement marking material, surface preparation, quality control tests, daily log, guarding devices, primer/adhesive, and glass beads.

Pavement markers will be measured in units of each for the type specified and will be paid for at the contract unit price per each.  This price shall include pavement cutting, surface preparation, primer if required, prismatic retroreflectors, adhesive, and castings.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Pavement message marking (Symbol or Text, Size, Type and Class) | Each or linear foot |
| (Type)Pavement marker (type pavement) | Each |

Section 704—PAVEMENT MARKINGS AND MARKERS of the Specifications is amended as follows:

Table VII-1 Pavement Markings is replaced with the following:

TABLE VII-1

Pavement Markings

| Type | Class | Name | Surface Temp. at Time of Application | Film Thickness (mils) | Pavement Surface | Application Limitations |
| --- | --- | --- | --- | --- | --- | --- |
| A |  | Traffic paint | 50°F+ | 15 1 when wet | AC HCC | May be applied directly after paving operations |
| B | I | Thermoplastic Alkyd | 50°F+ | 90 5 when set | AC HCC | May be applied directly after paving operations |
|  | I | Thermoplastic Hydrocarbon | 50°F+ | 90 5 when set | AC HCC | Do not apply less than 30 days after paving operations |
|  | II | Preformed Thermoplastic | 50°F+ | 120-130 | AC HCC | Manufacturer’s recommendations |
|  | III | Epoxy resin | 50°F+ | 20 1 when wet | AC HCC | Pavement surface needs to be at least 1 day old |
|  | IV | Plastic-backed preformed Tape | (Note 1) | 60 - 90 | AC HCC | Manufacturer’s recommendations |
|  | VI | Profiled preformed Tape | (Note 1) | (Note 1) | AC HCC | Manufacturer’s recommendations |
|  | VII | Polyurea | (Note 1) | 20 1 when wet | AC HCC | Manufacturer’s recommendations |
| D | II | Removable tape | (Note 1) | (Note 1) | AC HCC | Temporary (Construction) pavement marking |
| E |  | Removable Black tape (Non-Reflective) | (Note 1) | (Note 1) | AC | Temporary (Construction) pavement marking for covering existing markings |
| F | I | Temporary paint | (Note 1) | 40 max | AC HCC | Temporary (Construction) pavement marking |

Note 1: In accordance with manufacturer's recommendation.